## Slide 1: Optical Properties of Amorphous Nanolayers
Nicholas A. Kuhta
Oregon State University – Physics
kuhtan@onid.orst.edu
Oregon State University SSO Seminar 04/06/2010
Collaborators:
Bill Cowell (OSU Electrical Engineering)
Chris Knutson (OSU Chemistry)

## Slide 2
Outline:
Introduce Metamaterials/Plasmonics and discuss modern applications.
Overview fabrication and characterization of our bulk and
layered amorphous metal-dielectric metamaterials.
Show the optical properties of our structures – interesting conductivity
response, anisotropic, effective medium, hyperbolic dispersion.

## Slide 3
Controlling Light at the Nanoscale
DNA sensing -Gold nanoparticle
cluster size/dimension changes color.
Lee et. al Nano Lett. 9, 4564 (2009)
Roman Goblet from 4th century A.D.
Gansel et. Al Science 325, 1513 (2009)

## Slide 4
More Nano-Optics
Hoffman et. al Nature Materials (2007)
CNT photocurrent – Minot Group OSU
Pendry et. al Science 312 (2006)
IBM – FET with graphene channel (10GB/s)

## Slide 5
Metamaterial Application Goals:
Subwavelength imaging – beating the diffraction limit
Superfocusing – sub-diffraction
Cloaking – Super-absorbers (optical black hole)
Improved data storage via enhanced nanocontrol
High speed optoelectronic/photonic devices (Optical Computing)
New Sensor technology for Biological species
Dispersion Engineering (this work)
New Physics!!!
J. Lee - Acoustic Microscope
McGehee –
plasmonic
solar cells
Hulst –
Single molecule
nanoscale probe
Clark – split ring resonator

## Slide 6
Amorphous Metal Nanofabrication – DC Magnetron Sputtering
Cowell, Masters Thesis OSU (2010)
Experimental Technique:
Positively Charged Argon Plasma (color) – ejects atomic species from metal target.
Neutral ejected particles travel and are deposited on substrate in thin film form.
Pressure controls deposition rate (scattering)
Pros:
Uniform high deposition rate
Targets provide easy control of stoichiometry
Cons:
Requires vacuum apparatus
Targets:
ZrCuAlNi
TiAl3

## Slide 7
Dielectric Thin Film Deposition – Solution Spin Coating
Experimental Technique:
Inorganic aqueous-solution-processed oxide sample (ALPO)
Utilize surface tension to produce atomically smooth layers using spin-coating.
After the timed spin put on hot plate to remove water. (MOM bonds)
Knutson et. al (in preparation)
Pros:
Very inexpensive
Highly accurate – reproducible
Scalable
Cons:
Limited Material Set
Getting materials in solution

## Slide 8
TiAl3 – ALPO stack system
ZrCuAlNi – ALPO stack system
Cowell et. al Applied Materials
& Interfaces (2011)
TEM micrographs – Planar Metal-Dielectric Nanostructures

## Slide 9
Electron Diffraction Schematic
Speckled pattern = Crystalline Structure (long range spatially repeating order)
Diffuse pattern = Amorphous Structure (no structure - disordered)

## Slide 10
Amorphous Morphology – Electron Diffraction
Amorphous (no long range order)
single
crystalline

## Slide 11
Spectroscopic Ellipsometry - Reflectance
Measurement parameters:
Measure reflectance for angles between 20 and 80 degrees
Reflectance measurements range from 300nm to 1500nm
Both TE and TM polarization reflectance is measured
Negligible coupling between output TE and TM polarization states
Light-source:
Xe Lamp
(190nm-2400nm)
Xe Lamp Spectrum

## Slide 12
Single Layer (Thick Film) Reflectance - Ellipsometry
200nm - TiAl3
284nm - ZrCuAlNi

## Slide 13
Extracting Dielectric Response
In optically thick metals reflection only comes from the top interface
Note we’re using non-magnetic materials

## Slide 14
Palik,"Handbook of Optical Constants of Solids," Academic Press (luxpop.com)
Gold – Dielectric Response
Aluminum – Dielectric Response

## Slide 15
Palik,"Handbook of Optical Constants of Solids," Academic Press.
Copper – Dielectric Response
Titanium – Dielectric Response

## Slide 16
Bulk Dielectric Constants
Note the different response
for each metal!
As with all plasmonic
systems loss plays a
major role.

## Slide 17
Quasistatic Effective Medium Theory (Planar)
Due to the small thickness of
each material layer with respect to the laser wavelength (quasistatic) the material responds as an average anisotropic effective medium.

## Slide 18
isotropic
anisotropic
Anisotropic Dispersion Equation and Poynting Vector

## Slide 19
Anisotropic Dielectric Response – Effective Medium

## Slide 20
Multi-Layer Optical Reflectance – EMT Model
10 bilayers – 8nm (ZrCuAlNi), 8nm AlPO
10 bilayers – 4.7nm TiAl3, 11.3nm AlPO

## Slide 21
Error Analysis

## Slide 22
Acknowledgements
OSU Electrical Engineering:
William Cowell – (Sputtering Metal)
John Wager
OSU Material Science:
Brady Gibbons - Ellipsometry
OSU Chemistry:
Christopher Knutson – (Spin Coating Dielectric)
Doug Keszler
OSU Physics:
David McIntyre
Advisor:
Viktor Podolskiy

## Slide 23
Conclusions:
Ultra-thin nanostructures with atomically smooth interfaces reproducibly fabricated.
Bulk amorphous metals display interesting AC conductivity response.
Optical properties are consistent with anisotropic hyperbolic effective material response.
Applications and Outlook:
Dispersion Engineering (customized index of refraction)
Optical Filters
Subwavelength light compression
Waveguide systems
Stealth Coatings
Solar Cells (more than reflectors?)
Anisotropic Thermal Conduction